## Slide 1: Newell Highway Upgrade Project
28 km of Newell Highway
Single carriageway, single lane in each direction
Highest heavy vehicle traffic in NSW
Black soil country
Annual flood risk

## Slide 2: Regional Geology

## Slide 3: Scope of Investigation
DP provided:
  investigation services;
  factual reporting for submission to RMS; and
  laboratory testing.

## Slide 4: Scope of Investigation
114 Test pits (shoulder, embankment, verge, offline)
32 Pavement bores
12 Piezometers (with monitoring for 16 months)

## Slide 5: Scope of Investigation – Laboratory Testing
Subgrade
  CBR testing (4 day, 10 day and 21 day soak) – 105 tests;
  Atterberg limits – 71 tests;
  Particle size distribution including hydrometer – 24 tests;
  Emerson – 21 tests
  Acid sulfate testing – 50 tests
Pavement Materials
  CBR testing (4 day soak) – 16 tests
  Atterberg limits – 16 tests
  Particle size distribution including hydrometer – 16 tests;
Verge, Cutting and Bridge Sized Structures
  CBR testing (10 day soak) – 10 tests;
  Atterberg limits – 10 tests
  Particle size distribution including hydrometer – 10 tests;
  Emerson - 4 tests
  Acid sulfate testing – 45 tests
  Soil Aggressivity testing – 8 tests

## Slide 6: Scope of Investigation – Laboratory Testing
Subgrade
  CBR testing (4 day, 10 day and 21 day soak) – 105 tests;
  Atterberg limits – 71 tests;
  Particle size distribution including hydrometer – 24 tests;
  Emerson – 21 tests
  Acid sulfate testing – 50 tests
Pavement Materials
  CBR testing (4 day soak) – 16 tests
  Atterberg limits – 16 tests
  Particle size distribution including hydrometer – 16 tests;
Verge, Cutting and Bridge Sized Structures
  CBR testing (10 day soak) – 10 tests;
  Atterberg limits – 10 tests
  Particle size distribution including hydrometer – 10 tests;
  Emerson - 4 tests
  Acid sulfate testing – 45 tests
  Soil Aggressivity testing – 8 tests

## Slide 7: Scope of Investigation – Laboratory Testing
Chart: Number of Tests
| CBR | Atterberg | PSD with Hydrometer | Emerson | Acid Sulfate | Soil Aggressivity | Pinhole | Wet/Dry Strength | Resilient Modulus | UCS | Lime Demand | X-Ray Diffraction | Organic Content | Sulfate | Capillary Rise
Verge, Cuttings | 10 | 10 | 10 | 4 | 45 | 8
Pavement Blends | 8 | 6 | 8 | 8 | 2 | 9 | 9
Subgrade Blends | 6 | 6 | 34 | 9 | 3 | 3 | 3 | 6
Existing Pavement Materials | 16 | 16 | 16
Existing Subgrade | 105 | 71 | 24 | 21 | 50
130 – 1 per 200 m
Predominantly on subgrade
Subgrade lime stabilisation
Foamed Bitumen Stabilisation of Pavement

## Slide 8
Chart: 
| Existing Subgrade | Existing Pavement Materials | Verge, Cuttings | Pavement Blends | Subgrade Blends
Total Number of Tests | 271 | 48 | 87 | 50 | 70
Chart: 
| Existing Subgrade | Existing Pavement Materials | Verge, Cuttings | Pavement Blends | Subgrade Blends
CBR | 105 | 16 | 10
Atterberg | 71 | 16 | 10 | 8 | 6
PSD with Hydrometer | 24 | 16 | 10 | 6 | 6
Emerson | 21 | 4 | 8
Acid Sulfate | 50 | 45
Soil Aggressivity | 8
Pinhole | 8
Wet/Dry Strength | 2
Resilient Modulus | 9
UCS | 9 | 34
Lime Demand | 9
X-Ray Diffraction | 3

## Slide 9: Existing Pavement
40 mm to 50 mm AC
160 mm to 250 mm Base
100 mm to 300 mm Subbase (generally less than 200 mm)
Clay and Sandy Clay Subgrade
CBR = 8% to 45% (8 tests)
Clay and silt content = 17% – 23%
PI = 4% to 13%
CBR = 4.5% to 14% (8 tests)
Clay and silt content = 35% – 50%
PI = 5% to 17%
Shallow subgrade (30 tests)
CBR = 1.5% to 12%
Clay and silt content = 36% – 93%
PI = 18% to 59%
Deep Subgrade (20 tests)
CBR = 1.5% to 5%
Clay and silt content = 56% – 90%
PI = 31% to 49%
Poor quality base and subase material
Weak Subgrade

## Slide 10: What is foamed bitumen?
It is a mixture of air, water and bitumen
The characteristics include:
  Once a foaming agent is mixed, it expands about 15 times
  Large surface area and low viscosity
  When mixed with gravel material, the droplets coat the finer particles that binds them together

## Slide 11: What benefits?
Increases strength through stabilisation
Modulus increases significantly, shear strength gains (similar to that of cement treated material) but with higher flexibility
Higher flexibility reduces risk of fatigue (cemented material)
Decreases the permeability of the pavement
Less susceptible to heavy rainfall (i.e. copes with weather)
Sourced from Wirtgen Group, “Binder with a proven track record worldwide, foamed bitumen”
Unbound Pavement
Bitumen foam stabilised pavement

## Slide 12: What Disadvantages?
Not suitable for all pavements
Purpose built equipment needed
More expensive than other stabilisation methods

## Slide 13
Costs over $50k

## Slide 14: Where has it been done in Aus?
Queensland Main Roads
  1.6 km of Cunningham Highway at Gladfield (near Warwick)
  Gympie
  Inglewood

## Slide 15: Advantages for Pavement Design
The fatigue relationship for asphalt can be used in calculations (CIRCLY), as follows
  N = RF
  Where: N = allowable repetitions
  Smix = Modulus of foamed bitumen stabilised material
  VB = % by volume of bitumen in the stabilised material
  RF = reliability factor (=1 for rehabilitation)
This means greater allowable repetitions for the same thickness of pavement layers
RMS puts a cap on Smix of 2500 Mpa (close to some asphalts)

## Slide 16: Suitability Assessment
Differs for RMS and QMR
  RMS
    Binder (RMS R76)
    Foamed bitumen expansion ratio of 10 and minimum half life of 20 seconds
    Particle distribution as for Material to be bound (RMS 3051)
    Plasticity requirements (Austroads PI<10%) – lime can be added to reduce plasticity
    Test material with foamed bitumen to obtain average resilient modulus
    Plot the average resilient modulus against binder content to determine bitumen application rate require to satisfy table below

## Slide 17: Suitability Assessment
Chart: Foamed Bitumen Content (%)
| 2 | 3 | 4
Type 2.1 Gravel | 13270 | 10480 | 8470
Type 2.3 Gravel | 11330 | 9170 | 9310
Blend D - 25% pavement and 75% Type 2.1 Gravel | 11470 | 10080 | 10370
Minimum Soaked Modulus | 2000 | 2000 | 2000
Type 2.1 Gravel Initial Resilient Modulus | 540 | 635 | 530
Type 2.3 Gravel Initial Resilient Modulus | 700 | 585 | 595
Blend D - Initial Resilient Modulus | 1280 | 1420 | 1450
Minimum Initial Modulus | 700 | 700 | 700
Gravel 2.1 and 2.3 do not meet minimum initial resilient modulus
Blend D meets minimum initial resilient modulus and also minimum soaked resilient modulus

## Slide 18: Austroads Design Procedure for Foamed Bitumen
Long Term Modulus (based on laboratory trials)
Initial Modulus (needed because it is assumed that the road will be open within 3 hours of stabilisation)
Adjustments for climate, rate of load

## Slide 19
Then the following fatigue relationship is used in calculations (CIRCLY)
greater allowable repetitions for the same thickness of pavement layers
RMS puts a cap on Smix of 2500 Mpa (close to some asphalts)
Austroads Design Procedure for Foamed Bitumen

## Slide 20
Minimum Surface Requirements
< 1x107 ESA Spray seal or hot mix AC
≥ 1x107 ESA 30 to 40 mm AC (minimum)
Austroads Design Procedure for Foamed Bitumen

## Slide 21
Example
Austroads Design Procedure for Foamed Bitumen
Existing Road
(poorly performing)
Check Uncracked and cracked phase for bound base
Proposed Stabilised Road
5 x 106 ESA
300 mm
Reconstruction
(Austroads Mechanistic)
480 mm thickness
(Base and Subbase)
100 mm

## Slide 22
Remove about 300 mm
Lime stabilise remaining subbase and subgrade blend
Re-use top 300 mm with foamed bitumen stabilisation
Newell Highway Proposed Stabilisation

## Slide 23
Normal Stabilisation Process
  Run stabilised through the pavement (to stabilisation depth) to mix AC and basecourse
Foamed Bitumen Stabilisation Process
  Apply quicklime to the surface
  Slake quicklime
  Mix the slake lime through the pavement
  Shape and lightly compact
  Apply foaming agent to hot asphalt in tank and stabilise through pavement

## Slide 24
  Excavate to the proposed stabilisation depth
  Stockpile material
  Stabilise additional 300 mm of existing subbase and subgrade with 8% to 10% lime (LSF + 2%)
  Compact the stabilised material
  Place stockpiled material on exposed surface
  Apply quicklime to the surface
  Slake quicklime
  Mix the slake lime through the pavement
  Shape and lightly compact
  Apply foaming agent to hot asphalt in tank and stabilise through pavement
Proposed Newell Highway Stabilisation Process

## Slide 25: Lime Demand Test
Chart: Lime Content (%)
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
pH | 9.31 | 11.24 | 11.85 | 12.73 | 12.76 | 12.81 | 12.85 | 12.87 | 12.9
Hydrated Lime | 12.84 | 12.84 | 12.84 | 12.84 | 12.84 | 12.84 | 12.84 | 12.84 | 12.84
Measure the amount of lime to return mix to pH of Lime
This is the Lime Saturation Factor – (LSF)
Need to add more than the LSF before permanent modification of material occurs

## Slide 26: Testing Regime
Two Methods UCS v CBR
UCS testing of subgrade blends with lime
Trialled different mixes at LSF LSF+2, LSF+4
Lime, quicklime, hydrated lime
Aim to get UCS of 2.5 MPa @ 28 days
CBR testing on subgrade blends
Mixes at LSF, LSF+2, LSF+4
Aim to get increase in soaked CBR to allow improvement in thickness design and better support for foamed bitumen basecourse

## Slide 27: CBR Method
Subgrade 3.5%
Deep Subgrade 2.5%
Pavement Subgrade 3.5%
Offline Subgrade 4.0%
Overall Subgrade after 110 tests???
3%